# Surface-mounted internal louvre DucoGrille Close M100

Manufactured by: DUCO Ventilation & Sun Control

DucoGrille Close M 100 is a closable surface-mounted internal louvre manufactured from extruded aluminium sections. The plastic sliders provide adjustable ventilation. The DucoGrille Close M 100 is available as standard with heights of 200 or 300 mm and the width can vary up to a maximum of 1,000 mm.

## Features:

- Frame width: 13 mm

- Frame rebate: 20 mm

- Visual free area: 28 %

- Physical free area: 28 %

## Accessories (included):

- Fixing lugs

## Surface treatment:

- Anodisation: Qualanod-compliant, coating thickness 15-20µm, standard natural colour (colourless anodisation)

- Powder coating: Qualicoat Seaside type A compliant, minimum average coating thickness 60µm, standard RAL colours 70% gloss

Upon request: other finish coating thicknesses, anodising colours and paint gloss levels, textured paints and specific powder coating product codes

## Functional specifications:

### Flow rate:

  - K-factor inlet: 89.00

  - K-factor outlet: 89.00

  - Ce coefficient: 0.106

  - Cdcoefficient: 0.106

## Complies with or tested in accordance with the following standards:

- Qualicoat Seaside type A (if painted finish)

- Qualanod (if anodised finish)

- EN 573 - EN AW-6063 T66 and EN AW-6060 T66: aluminium alloy & hardening

- EN 13030: determination of Ce and Cd coefficients