# Solar shading system – DUCO Ventilation & Sun Control
DucoSun 150CF Underslung

## Description

DucoSun 150CF is an architectural component system with fixed louvres. Thanks to the patented DUCO “Slide-Click” system, the louvre blades are secured quickly and easily in a fixed angle to the support structure. The 150CF louvre blades combine the functional benefits of the basic 95C bladewith the attractive elliptical design of the DucoSun Ellips blade.

## Version

- Shape of blade	150CF

- Blade width		150 mm

- Blade height		30 mm

- Blade angle		60°

- Pitch			140 mm

- Blade length		Maximum 6000 mm

- Mullion		42/62

42/72

- Bracket		Both mullions can be combined with all brackets.

| Bracket | Decorative plate (optional) | Maximum shift |
| --- | --- | --- |
| 350/125/125 | 125/125 | 50 mm |
| 500/125/150 | 150/125 | 150 mm |
| 650/125/150 | 150/125 | 300 mm |

| Mullion | Facia (optional) | Strut |
| --- | --- | --- |
| 42/62 | 162 Flat | - |
| 42/72 | 175 Flat | Optional |

- Facia and strut

## Material and surface treatment

### Blades, mullions and facia

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness mullion: min. 2,5 mm

Profile thickness blade: min. 1,3 mm

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Clips

- Plastic			Polyamide PA 6.6 – glass fibre reinforced

### Brackets

- Steel			Hot-dip galvanised (50-60 μm)

Standard unpainted, decorative plate optionally available