# Solar shading system – DUCO Ventilation & Sun Control
DucoSun 95C Verticaal

## Description

DucoSun 95C is an architectural component system with fixed "C" louvres. Thanks to the patented DUCO “Slide-Click” system, the louvre blades are secured quickly and easily in a fixed

## Version

- Shape of blade	95C

- Blade height		71 mm

- Blade depth		71 mm

- Blade angle		45°

- Pitch			122,5 mm

- Blade length		Maximum 6000 mm

- Installation depth

| Mullion | Installation depth |
| --- | --- |
| 50/12 | 91 mm |
| 21/50 Multi | 129 mm |
| 30/50 | 129 mm |
| 50/50 | 129 mm |
| 42/62 | 141 mm |
| 42/72 | 150 mm |
| 50/125 | 204 mm |

## Material and surface treatment

### Blades and mullions

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 1,3 mm

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Clips

- Plastic			Polyamide PA 6.6 – glass fibre reinforced