# Solar shading system
DUCO Ventilation & Sun Control
DucoSun Cubic 100 Intermediate

## Description

Permanent external shading system made of aluminium. As standard, the blades are mounted at a fixed angle of 0° or 90° between coverplates. Project-specific assembly plates can also be worked out, creating a module. The plates are fixed between the supporting structure.

## Version

### Blade

- Blade type		Cubic 100

- Shape of blade	rectangular

- Blade height		100 mm

- Blade width		20 mm

### Plate

| Type | Inclination angle |
| --- | --- |
| Coverplate | 0° or 90° |
| Assembly plate | Project-specific |

### Blade fixation

- 4 x thread-forming screw DIN 7500-MZ M6 x 30

### Plate fixation

- The plates are provided with screw holes. For assembly plates, the screw holes may change according to the project.

- The blades with coverplates or modules are placed between the pre-assembled structure.

- Dilation is absorbed by neoprene washers.

### Material and surface treatment

### Blade

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 1.7 mm

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Plate

- Aluminium		AlMg3

Lasered, 5 mm thick

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

## Technical specifications

### Strength calculation

According to EN 1990, EN 1991, EN 1999