# Solar shading system
DUCO Ventilation & Sun Control
DucoSun Cubic 140 Moveable

## Description

Permanent external shading system made of aluminium with movable blades. The blades are mounted on site in the supporting structure (horizontally or vertically). The blades are continuously adjustable thanks to the linear electric drive motor.

## Version

### Blade

- Blade type		Cubic 140

- Shape of blade	rectangular

- Blade height		140 mm

- Blade width		37 mm

- Inclination angle	0° to 90°, continuously adjustable

### Mullion

- 60/100, fixing directly to the supporting structure

### Motor

- Power supply		230 VAC, 50 Hz

- Current		0.55 A

- Electric power		126 W

- IP class		IP65

- Cable length		2 m from actuator

### Accessories

- Aluminium stop for mullion 60/100 available

## Material and surface treatment

### Blade

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 1.5 mm

- Finish

  - Naturel anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Mullion

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 3 mm

- Finish

  - Naturel anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Coverplate

- Aluminium		AlMg3

Lasered, 5 mm thick

- Finish

  - Naturel anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

## Technical specifications

### Strength calculation

According to EN 1990, EN 1991, EN 1999