# Solar shading system
DUCO Ventilation & Sun Control
DucoSun Cubic Design 300

## Description

Permanent external shading system made of aluminium. The blades have a design surface texture and can be mounted at a fixed angle via coverplates at the end or with discreet wall brackets concealed in the back.

To create additional dynamics in the façade, optional LED strips can be integrated into the front of the louvres.

## Version

### Blade

- Blade type		Cubic Design 300

- Shape of lade		rectangle with ribbed surface

- Blade height		300 mm

- Blade width		68 mm

### Blade fixation

| Type | Inclination angle |
| --- | --- |
| Coverplate | 0°, 45° or 90° |
| Wall bracket | 0° |

### Accessories

- Optional LED strips available: white, colour (RGB) or white + colour (RGB).

  - White		11.52 W/m

  - RGB		12.8 W/m (2 per blade)

## Material and surface treatment

### Blade

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 2.5 mm

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Coverplate

- Aluminium		AlMg3

Lasered, 8 mm thick

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Wall bracket

- Steel			RVS 304

- Finish

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

## Technical specifications

### Strength calculation

According to EN 1990, EN 1991, EN 1999