# Solar shading system
DUCO Ventilation & Sun Control
DucoSun Ellips 100 Unifit

## Description

Permanent external shading system made of aluminium. The blades are mounted on site in the supporting structure (horizontally or vertically). The Ellips 100 blades are placed at a fixed inclination angle of 0° with a 'Unifit' fork. The elliptical louvre blades ensure the maximum amount of diffused daylight.

## Version

### Blade

- Blade type		Ellips 100

- Shape of blade	ellipse

- Blade height		100 mm

- Blade width		26 mm

### Bracket

- Type			Unifit

- Inclination angle	0°

- Height			80 mm

- Width			30 mm

### Blade fixation

- 2 x self-drilling screw DIN 7504-O Ø 4,8 x 16

### Bracket fixation

- Directly on supporting structure

  - 2 x self-drilling screw DIN 7504-O Ø 5,5 x 25

### Accessories

- Coverplates available

  - Aluminium AlMg3, lasered, 3 mm thick

## Material and surface treatment

### Blade

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 1.3 mm

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Bracket

- Aluminium		EN AW-6063 T66 (EN 573-3)

- Finish

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

## Technical specifications

### Strength calculation

According to EN 1990, EN 1991, EN 1999