# Solar shading system
DUCO Ventilation & Sun Control
DucoSun Ellips 250 Multifit

## Description

Permanent external shading system made of aluminium. The blades are mounted on site in the supporting structure (horizontally or vertically). The elliptical louvre blades ensure the maximum amount of diffused daylight.

Fastening is done with the patented Multifit system. This system consists of one base and a fork. The gearing between the two parts allows for 11 different positions. The inclination angle is adjustable during mounting.

## Version

### Blade

- Blade type		Ellips 250

- Shape of blade	ellipse

- Blade height		250 mm

- Blade width		43 mm

### Bracket

- Type			Multifit 80

- Inclination angle	-75°, -60°, -45°, -30°, -15°, 0°, 15°, 30°, 45°, 60° or 75°

- Height			90 mm

- Width			50 mm

### Blade fixation

- 2 x hexagon socket countersunk head screw DIN 7991 M5 x 55

- 2 x washer DIN 125-1A M5

- 2 x lock nut DIN 985 M5

### Bracket fixation

| Type | Material |
| --- | --- |
| Directly on supporting structure | - 1 x hexagon head bolt DIN 933 M8 x 20 - 1 x washer DIN 125-1A M8 |
| On DUCO mullion | - 1 x hexagon head bolt DIN 933 M8 x 20 - 1 x washer DIN 125-1A M8 - 1 x nut plate M8 |

### Accessories

- Coverplates available

  - Aluminium AlMg3, lasered, 3 mm thick

## Material and surface treatment

### Blade

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 1.5 mm

- Finish

  - Naturel anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Bracket

- Aluminium		EN AW-6063 T66 (EN 573-3)

- Finish

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

## Technical specifications

### Strength calculation

According to EN 1990, EN 1991, EN 1999